# DINITROL® RC 900

### Rust Converter (Epoxy Spray)

| Description: | Epoxy based rust converter with organic chelating agents. When dry it forms an impermeable barrier to oxygen and moisture effectively sealing out further corrosion. Hence, provides long-term resistance against corrosion and abrasion even under difficult conditions. |
| --- | --- |
| Colour: | Amber (Black when dry) |
| Typical Uses: | Conversion of corrosion on ferrous substrates into a stable organic iron compound. |
| Coating Characteristics: | Hard, dry film, which gives a good adhesion for corrosion prevention products or any commercially available topcoats and fillers. Penetrates approx. 7-10 times deeper into the rust pores than ordinary emulsion based rust converters |
| Application: | Remove all loose rust flakes; grease and dirt using a wire brush. Ensure that all grease and oil are removed with acetone or thinner. Shake the spray can well. Check substrate temperature is not below 10ºC. Hold spray can approx. 25 cm from surface to be treated. Apply two or three coats. Touch dry after one hour. Full drying time is between 2-6 hours depending on temperature, humidity and ventilation. A further layer can be applied after six hours. The product is best left overnight before applying other coatings. |
| Packages: | 400ml spray x 12 |
| Storage | Store between 5ºC and 40ºC. Protected from frost. Shelf life 72 months |
| Performance | Value |
| Type of film | Hard black when dry |
| Density at 23°C | 0.837 g/cm2 |
| Viscosity | 1.79 m2 |
| Solids content | 16% by weight |
| Flash point | 10°C |
| Drying time | 24 hours @ 20°C |
| Removal Agent | Before drying - | Water |
|  | After drying - | Acetone |
| Heat resistance | 180oC |
| Coverage | 66.7g per m2 |